폐식용유, 클링랩, 비닐봉투를 코팅하여 제조한

목재 브리켓의 내구성 및 내습성

양인1*, 이주남1, Peter Hall2, Martin Cooke-Willis2

(1서울대학교 그린바이오과학기술연구원, 2Scion)

Durability and moisture resistance of wood briquettes coated with used cooking oil, plastic cling-wrap and bag

In Yang1*, Junam Lee1, Peter Hall2, Martin Cooke-Willis2

(1Institutes of Green Bio Science & Technology, Seoul National University, 2Scion)

요약: 고형연료로서 재생가능한 자원인 목재의 사용은 연소시 화석연료와 비교하여 탄소중립적 성질을 보유하고 있어 기후변화의 주요 원인인 온실가스의 배출을 저감하게 된다. 목재를 이용하여 생산되는 펠릿 또는 브리켓과 같은 고체 바이오연료는 크기의 규격화를 통하여 생산설비의 대형화와 자동화가 가능해짐에 따라 유럽을 중심으로 사용량이 매년 크게 증가하는 추세이다. 그러나 목재자원의 지역적 편중으로 인하여 목재자원이 풍부한 지역에서 생산되는 목질계 고체 바이오연료는 해상운송을 이용하여 전세계적으로 이동되고 있다. 목재 브리켓은 고온에서 고밀화 과정을 통하여 제조되는 관계로 일정 수준 이상의 강도 및 형상을 유지하나, 외력이나 고습도와 같은 외부 조건에 의하여 목분 간의 결합력이 약화되고 결과적으로 품질과 상품성이 저하된다. 국내외적으로 브리켓의 강도 향상을 위한 많은 인자들의 적용이 시도되고 있으나, 내습성 향상과 관련한 연구는 미진한 실정이다. 따라서 본 연구는 목재 브리켓의 표면에 폐식용유, 클링랩, 폐기 비닐봉투의 코팅이 내구성 및 내습성에 미치는 영향을 조사하였다. 이 연구의 성공적인 결과는 방습을 위하여 비닐로 소포장되어 콘테이너 운송되는 시스템을 벌크선을 이용한 해상운송이 전환함에 따라 물류비용이 절감하게 될 것이다. 또한 폐식용유, 1회용 비닐봉투와 같은 페기물의 재자원화을 통하여 쓰레기 배출량의 감소에도 기여할 것으로 기대된다.

Abstract: When woody materials as a sustainable resource are used for fuels, the emission of greenhouse gas, which is a leading cause of the climate changes, can reduce comparing to fossil fuels due to its carbon-neutral property. The consumption of solid biofuels, such as wood pellets and briquettes has extensively increased, especially in EU, according to the enlargement and automation of production facilities with the standardization of the wood-based solid biofuels. However, owing to the unequal distribution of wood resources, wood-based solid biofuels produced in the countries having an abundant wood resources are globally shipped through the marine transportation. Wood briquettes have a certain level of strength and keep its own shape because it is produced through the densification process at a high temperature. However, bonding strength between wood particles in wood briquettes is weakened by the exposure conditions such as external forces and high humidity, and consequently the quality and marketability of the wood briquettes is deteriorated. Although the application of various factors has been tried to produce strong wood briquettes, few researches relating to the improvement of its moisture resistance were conducted domestically and internationally. Therefore, this research was carried out to examine how the coating of used cooking oil, plastic clingwrap and bag on the surface of wood briquettes affects its durability and moisture resistance. Sucess of this research makes the reduction of logistic cost by the utilization of bulk carrier instead of container carrier, which transports wood briquettes packaged by 20-kg plastic bags for the provision of moistureproof property. In addition, the reduction of waste discharge is expected by the recycling of municipal wastes, such as used cooking oil and disposable plastic bag.

Keywords: wood briquettes, durability, moisture resistance, used cooking oil, plastic clingwrap, disposable plastic bag