이태리포플러 목재칩의 연료 특성 분석에 관한 연구

정인선1*, 최윤성1, 조민재1, 문호성1, 오재헌1

(1국립산림과학원 산림기술경영연구소)

A Study on Analysis of Fuel Properties of

Populus canadensis Wood Chip

In-Seon Jeong1*, Yun-Sung Choi1, Min-Jae Cho1, Ho-Seong Mun1, Jae-Heun Oh1

(1Forest Technology and Management Research Center, National Institue of Forest science)

요약: 본 연구는 속성수인 이태리포플러를 에너지로 이용하기 위해 파쇄시기에 따른 목재칩의 연료특성을 분석하였다. 파쇄시기에 따라 목재칩 A(벌채 직후 파쇄)와 목재칩 B(현장건조 후 파쇄)로 구분하였으며, 목재칩의 연료 특성은 국립산림과학원에서 고시한 ‘목재제품의 규격과 품질기준(제2020-3호)’를 기준으로 분석하였다. 분석 결과, 목재칩 A와 목재칩 B의 질소와 크로뮴은 통계적으로 유의한 차이가 없는 것으로 분석되었으며(p>0.05), 크로뮴을 제외한 무기금속, 회분, 황은 통계적으로 유의한 차이가 있는 것으로 분석되었다(p<0.05). 또한, 목재칩 A는 겉보기밀도, 목재칩 B는 미세분 항목에서 목재칩 품질 기준에 만족하지 않아 모두 등급 외로 분석되었다. 파쇄 후 선별작업 적용 시 목재칩 크기의 균일화 및 미세분 감소 효과로 목재칩의 품질 향상이 가능할 것으로 판단되며 이에 대한 추가적인 연구가 필요할 것으로 사료된다.

Abstract: In this study, the fuel properties of wood chips were analyzed according to the time of chipping for use Populus canadensis, a species of short rotation coppice, as energy. The wood chip A(chipping immediately after harvesting) and wood chip B(chipping after on-site drying) were classified according to the chipping time. And the fuel properties were evaluated  based on the ‘Standards and quality standards of wood product (No.2020-3)’ announced by the National Institute of Forest Science. As a result of analysis of wood chip A and B, there was no statistical significant difference between nitrogen and chromium(p>0.05), and there was statistical significant difference in ash, sulfur, and inorganic substance excluding chromium(p<0.05). In addition, it was analyzed that wood chip A and B were not graded because of did not satisfy the standard of the bulk density and fines. It was decided that quality of wood chips can be improved by the effect of uniformity of the wood chips size and reducing fines, through the screening operation after chipping. Therefore, additional study on the effect of screening on wood chip quality are considered necessary in the future.

사사: 본 연구는 국립산림과학원 일반과제(FPO0200-2018-01)의 지원에 의해 이루어진 것임.