마이크로웨이브를 이용한 소나무재선충 피해목의 효율적인

살충처리시스템 개발(Ⅳ)

-시작기 시료테스트를 중심으로-

임희민1*, 김민규2, 권영두2, 전성화3, 최경수4, 박용호4, 기영오5, 박상준1

(1경북대학교 임학과, 2경북대학교 농업과학기술연구소, 3(사)경북대공학설계기술원, 4㈜삼익테크, 5포항시 산림조합)

The development of efficient insect killing system for the wood damaged by pine wilt disease using the microwave(Ⅳ)

-Focused on the sample test of prototype machine-

Hee-Min Lim1*, Min-Kyu Kim1, Young-Doo Kwon2, Seong-Hwa Jeon3, Kyung-Soo Choi4, Yong-Ho Park4, Young-Oh Ki5 and Sang-Jun Park1

(1Department of Forestry, Kyungpook National University, 2Institute of Agriculture Sciences & Technology, Kyungpook National University, 3Institute of Engineering Design & Technology, Kyungpook National University, 4Samictech CO., LTD., 5National Forestry Cooperative Federation, Pohang)

요약: 본 연구는 양질의 대경재 소나무재선충병 피해목을 다용도의 원목으로 이용하기 위하여 마이크로웨이브를 이용한 살충처리시스템을 개발하고자 제작한 시작기에 대한 시료테스트를 실시한 결과이다. 시작기는 Ø300⨯3,000(mm)의 소나무재선충 피해목 6본을 살충 처리할 수 있고, 채택된 마그네트론은 915MHz, 45kw이며, 피해목을 투입할 챔버는 1,320⨯3,195⨯1,326(mm)로서 시료목재 3본을 2단 적재하여 최대 6본까지 동시에 투입하여 살충 처리할 수 있다. 산림청의 소나무재선충병 방제지침은 마이크로웨이브를 이용한 소나무재선충의 사멸 인증기준으로서 피해목 벌채산물 전체에 최저 60℃에서 지속적으로 1분 이상 유지하여 처리하도록 되어 있다. 이를 기준으로 본 시작기 테스트에 사용된 시료는 직경 20∼30cm, 재장 1m의 소나무재선충병 피해 원목이고, 시료 깊이별 온도변화를 측정하기 위하여 원목에 천공한 후, 온도측정장치를 장착하여 온도변화를 측정하였다. 시작기의 시료 테스트 결과, 60℃에서 1분간 처리한 시료는 재선충이 생존하였으나, 3분 이상 처리한 시료는 재선충이 모두 사멸되었다.

따라서, 마이크로웨이브를 이용한 본 시작기에서는 소나무재선충병 피해목을 원목으로 사용하기 위해서 최소 3분 이상의 마이크로웨이브 주사 시간이 필요한 것으로 판단되었으며, 향후 목재의 함수율 및 직경별 살충테스트에 관한 추가 연구를 통해 효율적인 살충처리시스템을 구축할 수 있을 것으로 기대된다.

Abstract: In this study, we have tested the prototype machine designed and manufactured to develop the insect killing system using the microwave to use as a multipurpose log that the high quality and large diameter wood damaged by pine wilt disease. According to the guideline of Korea Forestry Service for the control of pine wilt disease, the certification standards of the death of pine wilt by microwave should be maintained the lowest at 60℃, continuously for longer than 1 minute throughout the harvested product. The prototype machine designed and manufactured on the basis of this, can input six pieces of Ø300-3,000(mm) of wood damaged by pine wilt disease, and adopted the magnetron of 915MHz, 45kw. The chamber for loading damaged wood is 1,320⨯3,195⨯1,326(mm) size. The method for loading damaged wood is designed to be able to simultaneously input up to 6 pieces of sample wood by loading 3 pieces of sample wood in two stages. The sample test was carried out with a temperature measuring device after perforating the wood damaged by pine wilt disease to measure the temperature change of depth with a diameter of 20∼30 cm, a length of 1m. As a result of the test with prototype machine, the pine wilts survived the samples treated at 60℃ for 1 minute. However, the pine wilts were completely dead in the samples treated for more than 3 minutes. On the basis of this, when treating wood damaged by pine wilt disease using microwave, it is believed that at least 3 minutes of microwave scanning time is required. In the future, it is expected that it will be possible to construct an efficient insecticide treatment system by carrying out complementary studies on insecticidal test according to water content and diameter of wood.

사사 : 이 연구는 산림청 ‘융복합기반 임산업의 신산업화 기술개발사업(2017094A00-1719-AB01)’의 지원에 의해 이루어 진 것임.