지역별 닥나무의 생육특성 및 수피율 분석

이소라*, 문보욱, 이형원, 김석주, 서정원

(국립산림과학원 산림바이오소재연구소)

Analysis of Growth Characteristics and Bark Yield of

Daknamu by Region

Sora Lee*, Bowook Moon, Hyung Won Lee, Seokju Kim, Jeong-won Seo

(Forest Biomaterials Research Center, National Institute of Forest Science)

요약: 닥나무(Broussonetia kazinoki)는 뽕나무과(Moraceae)에 속하는 낙엽활엽관목으로 국내에서는 그 인피섬유를 한지의 주재료로 사용한다. 최근 닥나무로 제작된 한지는 문화재 보존용지로 세계에서 인정받고 있으며, 문화재 복원뿐만 아니라 다양한 분야의 소재로 사용되고 있다. 그러나 닥나무 인피의 국내 생산량은 매년 감소하고 있고, 전통 한지 공방조차 원료를 구하기 어려운 실정이다. 이러한 문제를 해결하기 위해서는, 국내산 닥나무 공급 확대 방안 마련이 필요하다. 따라서 본 연구는 지역별 닥나무를 수집하여 한지원료 생산에 적합한 개체 선정을 위해 수행하였다. 닥나무는 생육이 정지된 겨울에 채취하여 길이, 두께(위, 중간, 밑), 주가지 생중량, 측아개수, 분지개수 등의 인자를 조사하고 흑피로 제조하여 개체당 수율을 분석하였으며, 인자 사이의 상관관계를 분석하였다. 그 결과 닥나무의 평균 길이는 240.10 cm, 가지 중간 두께 11.16 mm, 측아개수 약 36개, 분지개수 약 4개, 주가지 생중량 266.41 g, 그리고 흑피 수율은 26.14 g plant-1 로 나타났다. 상관관계 분석결과 수피 건중량은 가지 길이(r = 0.83), 가지 밑두께(r = 0.75), 주가지 생중량(r = 0.95)과 정의 상관으로 나타났으며(p < 0.01), 주가지 생중량은 개체당 수율과 강한 정의 상관으로 나타났다(r = 0.96, p < 0.01). 이와 같은 결과는 지역별 닥나무 간 차이가 있음을 나타내며, 닥나무의 생중량과 가지 밑 두께의 증가는 흑피 생산에 있어 긍정적인 효과가 있을 것으로 판단된다. 다만, 본 연구는 2023년 데이터로 다년간의 지속적인 연구가 필요하다.

Abstract: Daknamu (Broussonetia kazinoki), a deciduous shrub belonging to the Moraceae family, is primarily used in Korea for bast fibers, which are the main raw material for traditional Korean paper, Hanji. Recently, Hanji made from daknamu has gained international recognition as a preservation paper for cultural heritage and is also used in various other fields. However, domestic production of daknamu white bark has been decreasing annually, making it difficult even for traditional Hanji workshops to procure raw materials. It is essential to develop measures to expand the supply of domestically grown daknamu. Therefore, this study was conducted to collect daknamu from various regions and identify suitable specimens for producing Hanji. Daknamu samples were collected in winter when growth had ceased and investigated factors such as length, thickness (a top, middle, bottom), main branches fresh weight, number of lateral buds, and lateral branches. The yield per plant was analyzed by making black bark, and the correlations between various factors were studied. The results showed that the average length of daknamu was 240.10 cm, and the middle thickness of the branches was 11.16 mm, with approximately 36 lateral buds, 4 lateral branches, and a fresh weight of the main branches of 266.41 g. The black bark yield was 26.14 g per plant. Correlation analysis revealed a positive correlation between the dry weight of the bark and branch length (r = 0.83), branch base thickness (r = 0.75), and fresh weight of main branches (r = 0.95) (p < 0.01). Additionally, the fresh weight of the main branches showed a strong positive correlation with yield per plant (r = 0.96, p < 0.01). These results indicate variations among regional daknamu clones and suggest that increasing the fresh weight and base thickness of branches could have a positive effect on Heukpi production. However, this study is based on data from 2023, and continuous research over multiple years is necessary to draw more definitive conclusions.

사사: 본 연구는 국립산림과학원 연구과제 “우량 닥나무 생산 및 고품질 전통한지원료 전처리 기계화 공정 연구(과제번호 FP0802-2023-02-2024)”의 지원으로 수행되었습니다.