비파괴 음파 단층촬영법을 이용한 천연기념물(식물유산) 내부부후 평가

김광일1*, 김상미1, 안병석1

(1전라남도산림연구원)

Assessment of Internal Decay in Botanical Natural Monument Using Non-Destructive Sonic Tomography

Gwang-il Kim1*, Sang-mi Kim1, Byung-suk Ahn1

(1Jeollanamdo Forest Research Institute)

요약: 식물유산 천연기념물은 국가 자산으로서 희귀성, 고유성, 역사적 가치 등에 따라 미래에 온전하게 전승되어야 한다. 그러나 최근 이상기후에 따른 폭우, 강풍 등 비생물적 요인과 대량 발생하는 돌발 병해충 등 생물적 요인으로 인해 피해가 지속적으로 발생하고 있어 종합적인 관리대책이 필요한 실정이다. 특히 노거수 특성상 수목 내부의 부후 및 공동은 수목의 지지력 약화 등 구조적 기능 상실을 초래하기 때문에 내부 결함의 조기 발견을 통한 효율적 관리가 중요시 되고 있다. 그러나 식물유산 관리는 주로 조사자의 자체 육안평가를 통해 보호조치가 이루어지며, 내부부후도 측정의 어려움에 따라 그와 관련한 데이터는 매우 부족한 실정이다. 따라서 본 연구에서는 비파괴 내부진단 장비인 PiCUS3 Sonic Tomograph를 사용하여 식물유산 노거수의 현재 수목 내부 부후도에 대한 실증적인 데이터를 분석하고자 하였다. 대상수종은 낙엽활엽수(푸조나무, 느티나무) 3개소, 상록활엽수(후박나무, 동백나무) 2개소, 침엽수(곰솔, 은행나무) 2개소 등 총 7개소의 식물유산을 선정하였다. 측정 결과, 각각 예상결함면적비율은 푸조나무 75.9%, 느티나무 평균 89.7%, 후박나무 14.1%, 동백나무 0.1%, 곰솔 66.4%, 은행나무 83.2%로 나타났다. 대상수종 중 상록활엽수는 비교적 내부부후 진행이 심하지 않았으나 낙엽활엽수 및 침엽수에서 부후가 상당히 진행된 것으로 확인되어 향후 지속적인 모니터링을 통해 집중적이고 체계적인 관리가 필요할 것으로 판단된다.

Abstract: Botanical Natural Monuments constitutes national assets that should be preserved and transmitted intact to future generations based on their rarity, uniqueness, and historical value. However, in recent years, continuous damage has been occurring due to abiotic factors such as heavy rainfall and strong winds associated with abnormal climate conditions, as well as biotic factors including the large-scale outbreaks of invasive pests and diseases. Consequently, comprehensive management strategies have become increasingly necessary. In particular, as heritage trees are generally old and large, internal decay and cavities can lead to the loss of structural functions, such as reduced mechanical stability and load-bearing capacity. Therefore, efficient management through the early detection of internal defects is critically important. Nevertheless, current management of plant heritage relies largely on visual assessments conducted by investigators, and due to the difficulty of measuring internal decay, quantitative data on internal deterioration remain extremely limited. Accordingly, this study aimed to analyze empirical data on the current internal decay conditions of heritage trees using the PiCUS3 Sonic Tomograph, a non-destructive internal diagnostic device. A total of seven heritage tree sites were selected, including three deciduous broadleaf trees (Aphananthe aspera and Zelkova serrata), two evergreen broadleaf trees(Machilus thunbergii and Camellia japonica), and two coniferous trees (Pinus thunbergii and Ginkgo biloba). The results indicated that the estimated defect area ratios were 75.9% for Aphananthe aspera, an average of 89.7% for Zelkova serrata, 14.1% for Machilus thunbergii, 0.1% for Camellia japonica, 66.4% for Pinus thunbergii, and 83.2% for Ginkgo biloba. Among the target species, evergreen broadleaf trees exhibited relatively low levels of internal decay, whereas significant deterioration was observed in deciduous broadleaf and coniferous species. These findings suggest that continuous monitoring and focused, systematic management will be required in the future.

사사: 본 연구는 국가유산청 기후변화 대응 문화유산 보존관리 기술개발 사업(RS-2024-00397083)의 지원에 의해 이루어진 것임.